M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING
130 CARPET TILING:

Interface produces an extremely wide range of carpet tiles.  Tiles are available with tufted cut and loop pile, fusion bonded cut pile and micro-tuft and multi-level pile. Carpet tiles conform to the requirements of BS EN 1307. In addition to the supply of floor coverings, Interface also provides a routine carpet maintenance programme, using the Image range of cleaning materials. For further information contact Interface’s Technical Department.

Heuga 530 Carpet Tiles
A tufted plain textured loop pile tile, manufactured from 100% BCF Nylon with Graphlex® backing. 
Available in 24 colourways and carries a Class 33 heavy contract classification.
The 7.3mm thick tile is available in 500 x 500mm size as standard. Size options are available with minimum quantities.
Use our ReEntry service to take away existing Interface tiles which will be cleaned and repurposed through our ReEntry partners (Registered charities).

Simply add our Cool Carpet service to your order to make your purchase carbon neutral.

Consult with Interface for technical literature and to obtain samples.

Location: Heavy use areas. Office, retail, hospitality, leisure and educational areas.

Base: Please refer to Interface installation guide for details of suitability.

- Preparation: Subfloors should be prepared in accordance with BS 5325 or corresponding National and European Standards.

- Fabricated Underlay: Should be laid where required over existing timber bases.

Carpet Tiles:

- Manufacturer: Interface

- Product reference: Heuga 530 Carpet Tiles

- Type: Tufted plain textured loop pile

BS EN 1307 classification:

- Category: Type 1

- Level of use class: Heavy Contract 33

- Luxury rating class: LC2

Size: 500 x 500mm standard size. 
Colour/pattern: 5051 Zinc/ 5052 Smoke/ 5053 Carbon/ 5054 Twlight/ 5055 Silver/ 5056 Dolphin/ 5057 Basalt/ 5058 Black/ 5059 Sand/ 5060 Taupe/ 5031 Chocolate/ 5062 Volcano/ 5063 Ginger/ 5064 Garam Masala/ 5065 Orange/ 5066 Opera/ 5067 Santorin/ 5068 Cobalt/ 5069 Lobelia/ 5070 Blue Moon/ 5071 Lime/ 5072 Sycamore/ 5073 Ivy/ 5074 Midnight

Method of laying: Monolithic or Quarter Turn.

Interface Europe Ltd., Shelf Mills, Shelf, Halifax, West Yorkshire HX3 7PA

Tel: 01274 690690, Fax: 01274 694095.

Customer Services Tel: 08705 304030, Fax: 01274 698300,

Email: enquiries@interface.com     Web: www.interface.com